## Slide 1: Uncertainty Quantification for 2D Metamaterials
Han Zhang

## Slide 2: Input Parameters
Fixed Parameters:
  Geometry Design, a 10x10 Boolean Array with 1 indicating hard material, 0 indicating soft material.
Random Parameters:
  Soft material stiffness, E_soft, uniform distribution from 200e6±100e6
  Hard material stiffness, E_hard, uniform distribution from 200e9±100e9
  Soft material density, rho_soft, uniform distribution from 1e3±5e2
  Hard material density, rho_hard, uniform distribution from 8e3±4e3
  Soft material Poisson ratio, pr_soft, uniform distribution from 0.25±0.25
  Hard material Poisson ratio, pr_hard, uniform distribution from 0.25±0.25
Outputs of interest:
  Bandgap size
  Bandgap location
Input dimensionality has important implications for UQ computation. More on this in following slides.

## Slide 3: Dispersion Curve Calculations

## Slide 4: Histograms – 100 MC Inputs

## Slide 5: Histograms – 1000 MC Inputs

## Slide 6: Histograms – 10000 MC Inputs

## Slide 7: 7D Truncated Gaussian Distributions
E_soft: mean: 200e6 MPa, std: 8%
E_hard: mean: 200e9 MPa, std: 2%
Rho_soft: mean: 1e3 kg/m^3, std: 8%
Rho_hard: mean: 8e3 kg/m^3, std: 2%
Pr_soft: mean: 0.38, std: 2%
Pr_hard: mean: 0.28, std: 2%
Geo_fp: mean: 0.025, std: 8%

## Slide 8: Histograms – 7D Truncated Gaussian 100 MC Inputs

## Slide 9: Histograms – 7D Truncated Gaussian 1000 MC Inputs

## Slide 10: Histograms – 7D Truncated Gaussian 10000 MC Inputs

## Slide 11: The Geometry Uncertainty Problem
Curse of dimensionality limits possibilities with UQ on geometry.
Candidate approach: Individual Pixel Specification
  Treat each pixel as a separate input with some value between 0-1 representing a ratio of how much hard and soft material is in that pixel.
  Pros: Intuitive, simple, deterministic
  Cons: Input dimensions scales with pixel count
Candidate approach: Latent parameters w/ ML algorithms (Wei’s group)
  Use ML algorithms to generate realistic defects, forcing the neural architecture to be such that there are a small fixed number of “latent” parameters that specify the defect.
  Pros: Can be deterministic?, NN tunable to give certain types of defects preferentially
  Cons: Latent parameters are by definition not reflective of physical quantities, and thus difficult for any user to assign a distribution to given a real world problem.
Candidate approach: Edge pixel flip chance
  For any given geometry, locate subset of pixels that are at the edge between hard and soft materials. One value, the flip chance, is applied to all these pixels to get random flipping of pixels to generate defective shapes.
  Pros: 1D input regardless of geometry complexity, meaningful physical parameter
  Cons: NOT deterministic, which means this is only a valid geometry UQ approach if the distribution from geometry defects alone is small for any given flip chance, relative to the distribution from variations in material properties. I.e. all defects of a certain flip chance are similar in their impact on outputs of interest.
  Variations: Specify no. of flipped pixels instead of flip chance; include/exclude soft material from the edge pixel subset; count touching corners as edge pixels.

## Slide 12: Edge Pixel Flip Chance – Geometry Generation

## Slide 13: Finite Element Mesh Convergence

## Slide 14: Finite Element Mesh Convergence

## Slide 15: EPF (FC) – Defect Convergence
Typical bandgap size and center output distributions ranges 1000Hz for specified material property input distributions.
For 10p EPF, results are terrible, no way for any surrogate model to differentiate between effects of geometry defects and material properties.
However, around 40p, EPF becomes a reasonable strategy, with the distribution of computed bandgap results for fixed material properties and 100 randomly generated defective geometries being more than an order of magnitude tighter than ranges seen from UQ on material properties.
This suggests we may be able to either incorporate geometry defects as part of the original model (as a meta-parameter), or as one of the inputs to UQ.

## Slide 16: EPF (FP) – Defect Convergence
Typical bandgap size and center output distributions ranges 1000Hz for specified material property input distributions.
For 10p EPF, results are better with the FP approach than the FC approach. Still, we would probably consider this too wide of a distribution for any surrogate model to differentiate between effects of geometry defects and material properties.
However, around 40p, EPF-FP also converges and is a reasonable strategy, with the distribution of computed bandgap results for fixed material properties and 100 randomly generated defective geometries being more than an order of magnitude tighter than ranges seen from UQ on material properties.
This suggests we may be able to either incorporate geometry defects as part of the original model (as a meta-parameter), or as one of the inputs to UQ.

## Slide 17: EPF FC VS FP – Defect Convergence

## Slide 18: 7D Stochastic Collocation – Quadrature Rule – Bandgap Size

## Slide 19: 7D Stochastic Collocation – Quadrature Rule – Bandgap Top

## Slide 20: 7D Stochastic Collocation – Quadrature Rule – Bandgap Bottom

## Slide 21: 7D Stochastic Collocation – Quadrature Rule – Bandgap Center

## Slide 22: 7D Stochastic Collocation – MC Regression – Insufficient Sample Size

## Slide 23: 7D Stochastic Collocation – MC Regression (N = 1000) – Bandgap Size

## Slide 24: 7D Stochastic Collocation – MC Regression (N = 10000) – Bandgap Size

## Slide 25: 7D Stochastic Collocation – MC Regression (N = 1000) – Bandgap Top

## Slide 26: 7D Stochastic Collocation – MC Regression (N = 10000) – Bandgap Top

## Slide 27: 7D Stochastic Collocation – MC Regression (N = 1000) – Bandgap Bottom

## Slide 28: 7D Stochastic Collocation – MC Regression (N = 10000) – Bandgap Bottom

## Slide 29: 7D Stochastic Collocation – MC Regression (N = 1000) – Bandgap Center

## Slide 30: 7D Stochastic Collocation – MC Regression (N = 10000) – Bandgap Center

## Slide 31: Stochastic Collocation – Quadrature Rule
A variation of stochastic collocation where the orthogonal polynomials are fitted to specific points with weights, generated by using a rule function on the input distribution.
Extremely efficient at low dimensions, however points needed scales as s = (p + 1)^d, where s is the number of samples needed, p is the order of polynomial fit, and d is the dimensionality of the input space. This method therefore becomes very expensive very quickly as d increases.

## Slide 32: Stochastic Collocation – Quadrature Rule – Bandgap Size

## Slide 33: Stochastic Collocation – Quadrature Rule – Bandgap Center

## Slide 34: Stochastic Collocation – Quadrature Rule – Bandgap Top

## Slide 35: Stochastic Collocation – Quadrature Rule – Bandgap Bottom

## Slide 36: Stochastic Collocation – MC Regression
A variation of stochastic collocation where the orthogonal polynomials are fitted to MC generated samples
Usually more effective at higher dimensions and less efficient at lower dimensions compared to quadrature rule stochastic collocation

## Slide 37: Stochastic Collocation – MC Regression (Underfit)

## Slide 38: Stochastic Collocation – MC Regression – Bandgap Size

## Slide 39: Stochastic Collocation – MC Regression – Bandgap Center

## Slide 40: Stochastic Collocation – MC Regression – Bandgap Top

## Slide 41: Stochastic Collocation – MC Regression – Bandgap Bottom

## Slide 42: 1D PCE Fits
The following figures are for 1 input, 1 output scenarios, whereby the other 5 inputs are held at the following default values:
  E_soft: 200 MPa
  E_hard: 200 GPa
  Rho_soft: 1000 kg/m^3
  Rho_hard: 8000 kg/m^3
  PR_soft: 0
  PR_hard: 0.5

## Slide 43: 100, 1000, & 10000 MC E_soft & Bandgap Sizes

## Slide 44: 100, 1000, & 10000 MC E_soft & Bandgap Centers

## Slide 45: Stochastic Collocation 1D Quadrature – E_soft – Bandgap Size

## Slide 46: 100, 1000, & 10000 MC E_hard & Bandgap Sizes

## Slide 47: 100, 1000, & 10000 MC E_hard & Bandgap Centers

## Slide 48: Stochastic Collocation 1D Quadrature – E_hard – Bandgap Size

## Slide 49: 100, 1000, & 10000 MC Rho_soft & Bandgap Sizes

## Slide 50: 100, 1000, & 10000 MC rho_soft & Bandgap Centers

## Slide 51: Stochastic Collocation 1D Quadrature – rho_soft – Bandgap Size

## Slide 52: 100, 1000, & 10000 MC rho_hard & Bandgap Sizes

## Slide 53: 100, 1000, & 10000 MC rho_hard & Bandgap Centers

## Slide 54: Stochastic Collocation 1D Quadrature – rho_hard – Bandgap Size

## Slide 55: 100, 1000, & 10000 MC & Bandgap Sizes

## Slide 56: 100, 1000, & 10000 MC & Bandgap Centers

## Slide 57: Stochastic Collocation 1D Quadrature – – Bandgap Size

## Slide 58: 100, 1000, & 10000 MC & Bandgap Sizes

## Slide 59: 100, 1000, & 10000 MC & Bandgap Centers

## Slide 60: Stochastic Collocation 1D Quadrature – – Bandgap Size

## Slide 61: Histograms – Bandgap Top, Bottom, & Size

## Slide 62: Histograms – Bandgap Top, Bottom, & Center

## Slide 63: 2D Histograms

## Slide 64: Histograms – Bandgap Top, Bottom, & Size

## Slide 65: Histograms – Bandgap Top, Bottom, & Center

## Slide 66: 2D Histograms

## Slide 67: 2D Histograms

## Slide 68
E_soft
E_hard
Rho_soft
Rho_hard
Pr_soft
Pr_hard